## Slide 1: Robust Origami Containers
Harvard BioMod 2011

## Slide 2: Goal
To create DNA origami containers that can load, hold, and release cargo
To do this, we must:
  design and fold robust 3D origami featuring enclosed interiors with optimized volumes
  design and implement mechanisms that allow us to controllably:
    load cargo by attaching it to the inside of a container
    close the container
    solubilize cargo without leakage to the exterior of the container
    open our container, releasing our cargo

## Slide 3: Current Designs
Container
  Sphere
  Box with lid
Cargo
  5 nm gold particles
  DNA/RNA strands

## Slide 4: Sphere
D. Han et al., Science 332, 342 (2011)

## Slide 5: Disulfide Crosslinks: Solubilization

## Slide 6: Disulfide Crosslinks: Opening Mechanism

## Slide 7: Strand Displacement: Opening Mechanism

## Slide 8: Restriction Enzyme: Opening Mechanism

## Slide 9: Testing the Restriction Enzyme Design

## Slide 10: Visualization With SphereCAD
3D rendering assists in experimental synthesis of spherical origami
Maya 3D
caDNAno

## Slide 11: Desired SphereCAD Function
Through creation and execution of scripts:
  Highlight helix #, scaffold position of selected base
  Convert spherical coordinates to pairs of helix # and scaffold position
  Jump to any position on sphere based on user input
  Draw nanoparticles on sphere surface
  Determine whether placement agrees with base orientation

## Slide 12: Box with Lid

## Slide 13: CanDo Interpretation

## Slide 15: Minimal Box Test

## Slide 16: Preliminary Experiments
Disulfide crosslinking
Nanoparticle conjugation
Nanoparticle chain

## Slide 17: Nanoparticle Chain: World’s Smallest Necklace

## Slide 18: Annealing Handles to Ultramer

## Slide 19: Making 5 nm Gold Nanoparticles
Heat aqueous gold chloride to 60°C
Add solution of citrate (stabilizer), tannic acid (reducing agent), potassium carbonate (pH adjustment)

## Slide 20: Characterizing Nanoparticles

## Slide 21: Making 15 nm Gold Nanoparticles
Heat aqueous gold chloride to 95°C
Add citrate (stabilizer and reducing agent)

## Slide 22: Characterizing Nanoparticles

## Slide 23: Making Larger Nanoparticles
Use 5 nm particles as seeds
Vary amount of seed solution
Add gold chloride
Add citrate
Produce ~50-150 nm gold particles

## Slide 24: Characterizing Nanoparticles
500 uL of 5 nm seeds

## Slide 25: Characterizing Nanoparticles
200 uL of 5 nm seeds

## Slide 26: Characterizing Nanoparticles
50 uL of 5 nm seeds

## Slide 27: Characterizing Nanoparticles
20 uL of 5 nm seeds

## Slide 28: Characterizing Nanoparticles
5 uL of 5 nm seeds