PDMS (Polydimethylsiloxane) & PS (Polystyrene) 2D MATRIX

PDMS

- Tare vial on scale, fill vial half way with Syland 184. Add Elastomer Curing Agent to produce a 20:1 concentration (use glass pipette when added curing agent)

- Use bunt end of pipette to mix, mix till confluent in bubbles

- Place vial in gas chamber, turn chamber on let bubble till it reaches the top. Turn off gas and let sit till all the bubbles evaporate

- Pour liquid PDMS onto silicon wafer with photolithography template and O-ring

- Place silicon wafer/PDMS in 70◦C oven o/n

*Use contact-adhesion to test modulus of PDMS

*Change concentration (10:1, 20:1) of PDMS for softer PDMS

Spin Coat PS

- Wash silicon wafer with soap and water, use forceps when handling wafers at all times

- Dry wafer under hood then wash with Toluene 1X, dry

- Wash with Isopropanol 1X, dry

- Place wafers on glass slide in UVO oven, run oven for 10mins (add time to counter)

- Turn spin coat machine on, release air valve, make sure “T” is facing clean on spin coat motor

- Place wafer onto spin coater, select VACUM, PROGRAM to set 3000rpm for ~45sec, 1 cycle

- Add PS/Toluene solution to wafer, cover ~90% for maximum efficiency

- Select F10 to display OFF, select START/RUN to begin spin coat

- Select VACUM when complete

*Higher rpm or vary [ ] of PS to change thin/thickness of PS

*Use interferometer to measure thin/thickness of PS

*PS can be stored at room temperature

Combining PDMS and PS

- Take PDMS out of oven, cut around O-ring with a razor, flip PDMS upside down so template side is facing up (use black table top to cut and see template)

*PDMS can be stored at room temperature

- Cut squares to fit into designated well plate

- Transfer PDMS onto wafer with PS template facing down on PS

- Cut PS lightly to form a border around the PDMS

- Use water bath to float PDMS/PS off of wafer, use forceps for help

- Once PDMS/PS is floating in water, use forceps to place device onto appropriate slide/well film should be facing up

*PDMS/PS plates can be stored at room temperature

PLASMA TREATMENT

- Check liquid Nitrogen container to make sure it is at an appropriate level

- Place slide/plate in chamber, close door and turn red lever “close”

- Make sure “valve” switch is on and “power” switch is off

- Watch vacuum gauge, when it reaches 150-200 release oxygen valve, repeat 2xs

- During final vacuum pump, slowly release oxygen valve to keep vacuum pump at 150-200

- Turn on “power” switch and set to “HI” setting

- Run for 10 minutes, should be reddish/purple in color

- When time is completed turn of “HI” first then turn “power” switch off

- Turn red lever “close” to open, release oxygen slowly and door will open

- Use forceps to take sample out and place in the appropriate sterile dish