## Slide 1: Biomaterials and Cell-Biomaterial Interactions
Module 3, Lecture 2
20.109 Spring 2014

## Slide 2: Lecture 1 review
What is tissue engineering?
Why is tissue engineering?
Why care about cartilage?
What are we asking in Module 3?

## Slide 3: Topics for Lecture 2
Introduction to biomaterials in TE
  properties
  examples
Cartilage composition
  collagen
  proteoglycans
  structure  function

## Slide 4: Today in Lab: M3D2
1 condition per plate (2 plates total)
2 wells per plate (split 1 mL of beads)
if contaminate 1 well on D3, still have 1 on D4
0.5 mL beads, 6 mL media
0.5 mL beads, 6 mL media
Condition 1 of 2

## Slide 5: Properties of biomaterials
Physical/mechanical
  strength
  elasticity
  architecture (e.g., pore size)
Chemical
  degradability
  toxicity
  water content
Biological
  motifs that cells recognize
  release of soluble components
Lifetime
O
OH
OH
O-
O

## Slide 6: The right material for the job
Metals
  Ti, Co, Mg alloys
  pros: mechanically robust
  applications: orthopedics, dentistry
Ceramics
  Al2O3, Ca-phosphates, sulfates
  pros: strength, bonding to bone
  applications: orthopedics, dentistry
Polymers
  diverse, tunable properties
  applications: soft tissues
http://www.weisshospital.com/joint-university/hip/metal.html
Metal hip implant
General: B. Ratner, ed. Biomaterials Science, 1996.
Bone
Si-HA
Image: Porter et al., Biomaterials 25:3303 (2004).
Interface
Notes: Silicate-hydroxyapatite mix vs. plain HA in bone  mechanical interlocking (chemical bond not needed, additional) b/w collagen fibrils and the Si-HA.

## Slide 7: Basics of polymer structure
Linear polymers
  repeated chemical unit, or
  heterogeneous repeats: co-polymer
Homo- example: PEG
  synthesis: epoxide ring-opening
  adds one monomer at a time
Co- example: PLGA
  successive ester bonds formed
  also by ring-opening!
  Many types of linear syntheses
As MW increases
  entanglements and strength 
  processability 
Poly(ethylene glycol)
Poly(lactic-co-glycolic acid)
[public domain image]
(
)
OH
O
H
n

## Slide 8: Polymers are diverse and tunable
Chemical groups affect
  mechanical properties
  stability/degradability
  hydrophilicity
  reactivity/modification ease
  gas permeability
PEG
  unique relationship with water
  resists protein adsorption
  low MW easily excreted
PLGA
  ester bonds hydrolyzed
  PLA more hydrophobic and degrades more slowly cf PGA
Poly(ethylene glycol)
Poly(lactic-co-glycolic acid)
[public domain image]
(
)
OH
O
H
n
Notes: PEG: mix of hydrophilic/hydrophobic, special relationship with water (H-bonds with O; coil structure), low MW easily excreted, resists protein adsorption
PLGA: ester links water degradable; very hydrophobic (drug delivery issues); PGA more crystalline, degrades faster than PLA; acidity issues, but overall safe
Low MW point is for drug capsules; note also PEGylation for slower protein drug clearance (lower immunogenicity)

## Slide 9: Network polymer synthesis example
Network structure
  covalently cross-linked chains
  water-swollen (if hydrophilic)
=
=
=
*
=
Network polymer
*
=
=
radical
*
UV
+ initiator
=
=
Linear polymer with reactive end groups:
=
acryloyl
=
=
Notes: Contrast covalent cross-links with physical entangmlements
CH2CHCOR http://en.wikipedia.org/wiki/Acryloyl_group the CH and the CO both sites for radical formation
MAYBE ORALLY MENTION ANOTHER APPROACH?

## Slide 10: Properties of hydrogels such as PEG
Mimic soft tissues
  water content
  elasticity
  diffusivity
Synthesis at physiological conditions
  temperature
  pH
  UV light: spatio-temporal control; safe; patterning potential
Injectability
Chemical modification
(Stachowiak & Irvine)
Review: Nguyen KT & West JL, Biomaterials 23:4307 (2002)
Notes: MORE RECENT REVIEW?
ADD A SLIDE HERE WITH A MORE RECENT PATTERNING ETC EXAMPLE? OR ADDED MATERIAL FOR LECTURE 3? WAIT FOR LEC 3

## Slide 11: Materials must be biocompatible
Avoid bio-incompatibility
  chemical toxicity: cells, genomes
  immunogenicity
  protein/cell adhesion  clotting
  bacterial adhesion
Material properties
  material and its degradation products non-toxic and non-immunogenic
  resistance to protein adhesion
  Sterility
PEG is a great bioinert material
Normal artery
Occluded artery
Data from: Zavan B, et al., FASEB J 22:2853 (2008).
Notes: Large vessels (4mm) in porcine model; some occlusions.
Vascular TE. Research gap is proper ECM (esp elastin) biosynthesis.
2010: “Nonetheless, a durable small-caliber (diameter: <6 mm) conduit remains elusive, and patency rates for infrainguinal revascularization through the use of a prosthetic graft have changed little over the past 30 years. “ “insufficient or noncrosslinked elastin” “Unlike collagen, the stable crosslinked fiber network of native elastin makes isolation and purification techniques difficult. “
2006: “elastin: the missing link”

## Slide 12: Beyond bioinert: bioactive materials
Attach proteins/peptides for
  specific cell adhesion
  degradability
Release cytokines for
  proliferation
  differentiation
  attraction
e.g., West JL and Hubbell JA Macromolecules 32:241 (1999)
Fibroblasts on polymer-peptide gels (Stachowiak).

## Slide 13: Interlude: scientific misconduct
Sources
Nature News
03/18/14
Boston Globe
04/09/14
Notes: NOTE: WAS REPRODUCILITY; ALSO RECENT P-VALUE STUFF ON MTMB COULD BE INTERESTING

## Slide 14: Natural vs. synthetic polymers
Natural pros/cons
  built-in bioactivity
  lot-to-lot variation, unpredictable
  poor mechanical strength
  immunogenicity (xenologous sources)
Synthetic pros/cons
  predicting biocompatibility is tough
  mechanical and chemical properties readily altered
  minimal lot-to-lot variation
Synthetic advantages: tunable and reproducible
Notes: [S13 EXAMPLES SLIDE? OR NEW LEC3 MTL (STATS GONE)]

## Slide 15: Revisiting cartilage structure
boundary with bone
chondrocytes
cartilage surface
collagen fibers
proteoglycans
Water-swollen, heterogeneous, avascular and cell-poor tissue.

## Slide 16: Structure of collagen(s)
1° structure:
  Gly-X-Y repeats
  proline, hydroxyproline
3° structure: triple helix
  Gly: flexibility
  Hyp: H-bonding
4° structure: fibrils
  many but not all collagens
  cross-links via lysine, hydroxylysine
  periodic banding observable
Molecular image made using Protein Explorer (PDB ID: 1bkv).
Fibril image from public domain.
HYP residues
E. Vuorio & B. de Crombrugghe Annu Rev Biochem 59:837 (1990)
Notes: Fibrils can be homo and heterotypic. Banding occurs because of consistent gap between chains (40 nm horizontal gap, 67 nm overlap hence darker, each 300 nm long). Called “quarter-stagger” array.

## Slide 17: Macro structure of fibrillar collagen
A. Stachowiak and D.J. Irvine, confocal reflection microscopy of collagen-filled synthetic scaffold.
PEG scaffold:
microporous (bead template)
strict order
CN filler:
nanoporous
apparent disorder

## Slide 18: Collagen composition in cartilage
D.J. Prockop Annu Rev Biochemritis Res 64:403 (1995)
D. Eyre Arthritis Res 4:30 (2002)
Collagen types vary in
  location
  glycoslyation
  higher-order structure
  homo- (II) or hetero- (I) trimers
Cartilage collagens
  Type II with IX and XI
  exact roles of IX and XI unknown
    inter-fibrillar cross-links
    modulate fibril diameter
    integration with rest of ECM
  others(III, VI, X, XII, XIV)
Little collagen turnover in adult cartilage
D. Eyre (2002)
CN II
CN XI
CN XI
Notes: Mutations to II, IX, XI cause disease. Specifically, IX may help coordinate insertion of PGs etc. in the ECM and XI big role in determining diameter (even if IX not present).
CN III may play a role in wound healing/matrix remodeling. Support roles for the non-II’s, essentially.
“Our results show that type IX collagen and COMP are involved in matrix assembly by mediating the anchorage and regulating the distribution of other matrix macromolecules such as proteoglycans and matrilins and have counteracting effects on collagen fibril growth. Loss of type IX collagen and COMP leads to matrix aberrations that may make cartilage more susceptible to degeneration.”

## Slide 19: Proteoglycans are bulky and charged
Chondroitin sulfate
(public domain image)
PG: proteins with GAG side chains
  GAG is glycosaminoglycan
  many charged groups: COO- , SO3-
  electrostatic repulsion
Main cartilage PG is aggrecan
  GAG is primarily chondroitin sulfate (CS)
  aggrecans polymerize via hyaluronin (HA)
Aggrecan monomer
HA-binding
CS chains
R.V. Iozzo Annu Rev Biochem 67:609 (1998)
Notes: POISED TO GET IT CAUSE M2: Multiple globular domains, can distinguish on Western. Some may be cleaved off by aggrecanases, want to know if have full-length or not. LP = link protein. Lectin domain can bind sugars, may connect different cell/ECM components.

## Slide 20: PG form aggregates of varying sizes
Monomer > 1M, aggregates > 100M Da
Average size decreases
  with age
  with osteoarthritis (OA)
Aggrecenase inhibitors may be an OA target
High negative charge density leads to osmotic swelling
Aggrecan aggregate
HA
C.B & W. Knudson Cell & Dev Bio 12:69 (2001)
CS chains
CS chains
Notes: Review osmotic swelling: PG high charge density thus need high positive ion influx, and subsequently water wants to come in due to [ion] difference.

## Slide 21: Macro structure of the knee
See also movie:http://orthoinfo.aaos.org/topic.cfm?topic=a00212
Requirements of a joint
  load transfer
    bone/bone
    bone/muscle
  flexibility
    synovial fluid lubricates
http://orthoinfo.aaos.org/topic.cfm?topic=a00212
Healthy knee
OA
knee
Notes: Review osmotic

## Slide 22: Cartilage structure and function
Cartilage composition
  dry weight: CN 50-75% ; PG 15-30%
  water: 60-80%
  cells: 5-10% (v/v)
Role of PG
  high compressive strength (osmotic swelling)
  low permeability and high drag coefficient reduce wear on joint  H2O bears some load
Role of CN
  high tensile strength (~GPa)
  contain swelling forces of PG
V.C. Mow, A. Ratcliffe, and S.LY. Woo, eds. Biomechanics of Diarthrodial Joints (Vol. I) Springer-Verlag New York Inc. 1990
cartilage
synovial fluid
bone
bone
Notes: Review osmotic swelling: PG high charge density, but packed close/constrained by CNII. Thus need high positive ion influx, and subsequently water wants to come in due to [ion] difference. CN again constrains the swelling behaviour.
Under compression, water is excluded, but low permeability and high drag coefficient mean it is hard to remove water and thus it bears the load, and permeability further decreases as some water leaves. OA degradation means that more water comes in and increases permeability. Latter increase means less load is shared by the fluid.

## Slide 23: Principles of osmotic pressure
Water must have equal chemical potential in both compartments: μH2O,1 = μH2O,2
Solutes decrease μ, pressure increases μ
Infinite water would equalize [solute], but influx limited
Charges must also be balanced (Donnan equilibrium)
H2O + high [Na+]/PG-
H2O + low [Na+]
1
2
Simplified cartilage model
Membrane:
PG can’t cross
Notes: If water is constrained from entering compartment 1 to equalize solute concentrations, an excess pressure in compartment 1 makes for equal μ  hence compressive strength

## Slide 24: Poor water retention in OA cartilage reduces load sharing, increases wear
Simplified cartilage model
Image: DA Binks et al., Br J Radiol 86:20120163 (2013).
Notes: REVIEW THIS ONE

## Slide 25: Lecture 2: engineered and native biomaterials
Diverse biomaterials are used in TE.
Cell-material interactions can be (+), (-), or neutral.
Hydrogels are useful for soft tissue engineering: similar properties and easily tunable.
The composition of cartilage supports its functions.
Next time… cell viability and imaging; intro to standards in scientific communities.