Slip Preparation and Seeding

Materials

Cover Slips

Liquid Nitrogen

APTES

Mineral Oil

Toluene

Ethanol

Nanopure Water

DSC

DIEA

Dry Acetone

PBS

Long (24) PEG

Cells

Media

Procedure

- Plasma treat

  - Make sure there is liquid nitrogen in the glass well covered in cloth

  - Place slips in 12 well plate, 2 per plate leaning against each other like this:  \/

  - Open red lever in back, point black lever down in front, push door shut

  - When the gauge reads less than 200 millitorr turn power on, RF to high, open yellow knob slightly. If it’s working plasma will be purple. Treat 10 minutes

  - To finish, close O2, turn off RF, turn off power, close red lever, and point black lever up. Leave on vacuum pump and pump switch

- APTES (same day as plasma treatment)

  - Dry slips and evaporation tube in vacuum oven at 110 C for 10 minutes

  - Heat mineral oil to 90 C on hotplate with stir bar (best to start before plasma treatment so it’s hot by the time you get back)

  - Measure .5 mL of APTES into the tube, place in slips, allow to react overnight

- Wash slips

  - Wash in a 500 mL glass beaker with roughly 200 mL of toluene followed by ethanol and then nanopure water

  - Dry in vacuum oven overnight under N2

- DSC treatment

  - React with .3 g DSC, 1mL DIEA, and 29 mL dry acetone (for 9 slips, increase for more slips) for 2 hours on shaker at 75-90 rpm

  - Wash with acetone 3 times and dry overnight under N2

- Functionalizing:

  - make appropriate dilutions of functionalizing protein

  - Place wet paper towels and beakers of water into plastic bin. Place glass plate over wet paper towels and cover with another wet paper towel. Place parafilm on top

  - Place 100uL of solution onto parafilm and place slip overtop, allow to react for 3 hours covered in foil

  - Wash 4 times with PBS

  - Block with 10 ug/cm2 Long PEG for 2 hour

  - Wash 4 times with PBS, store in fridge in PBS overnight if not using immediately

- Seeding cells

  - Sterilize slips by placing 12 well plate in hood, open, for 30 minutes under UV light

  - Seed cells at 10,000 cells per well (2 mL media for 12 well plates, 3 mL media for 6 well plates)