COMPREHENSIVE PEG-PC GEL PROTOCOL

Last updated 2/4/2013 by W.H.

MATERIALS

# 2-Methacryloyloxyethyl phosphorylcholine (Sigma)

# Poly(ethylene) glycol dimethacrylate, MN ~ 750 (Sigma)

# PBS

# 0.22 µm PES syringe filters

# Luer-lock syringes

# microcentrifuge tubes

# vortexer

# For UV curing: Irgacure 2959 (Ciba), a high-intensity UV light source, methacrylate silane-treated coverslips and Sigmacote-treated coverslips

# For thermal curing: ammonium persulfate and TEMED (Bio-Rad), vacuum oven/chamber, N2 gas, methacrylate silane-treated glass-bottomed 96-well plates

PREPARATION OF PRE-POLYMER SOLUTION

- Make a solution of 20% (w/v) MPC in PBS i.e. 200 mg MPC per mL of PBS (actual w/v after volume change is ~17%) and vortex to dissolve. Calculate the volume to make on a basis of 75 µL pre-polymer solution per coverslip or 40 µl/well in a 96-well plate.

- Evenly distribute 20% MPC solution into microcentrifuge tubes for each PEG-PC concentration to be made.

- Add the appropriate amount of PEGDMA. For example, if making 3% PEG-PC and you measured out 300 µL of 20% MPC, add 3% of that volume as PEGDMA i.e. 0.03 * 300 µL = 9 µL of PEGDMA. Mix thoroughly by vortexing. (N.B.: If making PEG-PC over 10%, the % of MPC and PEGDMA is calculated differently because the volume changes are substantial).

- If gels are to be used for cell culture experiments, syringe filter each solution.

- Degas each solution with ultrapure (grade 5) N2 for ~30 seconds (this is especially important for thermal curing). Be sure to sterilize the degassing needle with 70% ethanol to keep the solutions clean, and run ethanol through the needle when finished so it does not get clogged.

POLYMERIZATION ON COVERSLIPS

- Make fresh 20% w/v Irgacure 2959 in 70% ethanol, vortex to dissolve (it takes a lot of vortexing). Degassing this solution is not usually necessary, but it cannot hurt.

- Add 40 µL of 20% Irgacure per 1 mL of polymer solution. Mix gently, by inverting or pipetting, so as to not reintroduce dissolve oxygen into the solution.

- Place 75 µL aliquots of pre-polymer solution on methacrylate silane-treated cover slips. Carefully cover with a Sigmacote-treated cover slip.

- Treat with UV at 5-6” distance for 7 minutes.

- Carefully remove the Sigmacote coverslip with fine forceps.

- Store the gels in PBS overnight.

POLYERMZATION IN 96-WELL PLATES

- Make fresh 20% ammonium persulfate (APS) in deionized water, vortex to dissolve. Degassing this solution is not usually necessary, but it cannot hurt.

- To polymerize, add 20% APS to pre-polymer solutions at a 1:80 ratio, and add TEMED 1:800. i.e. 1000 µL pre-polymer / 80 = 12.5 µL 20% APS and (1000/800) = 1.25 µL TEMED. N.B.: After addition of APS and TEMED it is possible for the solution to polymerize on the bench top, so it is recommended that each PEG-PC concentration be done separately i.e. don’t add APS and TEMED to every pre-polymer solution before aliquoting into wells.

- After addition of APS and TEMED, aliquot 40 µl/well into the wells of a methacrylate silane-treated 96-well plate.

- Repeat for every PEG-PC concentration being made.

- Place 96-well plate in vacuum oven at room temperature with the cover off and flow ultrapure (grade 5) N2 at 25 psi through the chamber for 5 minutes.

- After 5 minutes of flowing N2, close the inlet and outlet to the vacuum oven tightly and close the N2 valve.

- After 5 additional minutes, gels should have formed.

- Swell in PBS overnight. Use 100 µl/well, except for 0.5% PEG-PC gels use 200 µl/well (because they swell so much).