Lab Plans and Actions for Week 7/21/08-7/27/08
	Scientist
	Report (7/21-7/27)
	Plans (7/28-8/3)

	Jane

Zhang
	· AFM on old SERS sample during training
· Observed 2 different morphologies on sample surface, heights: 80nm and 10nm 

· suspect bigger particles to be gold, and smaller and denser ones to be dried SiO2 substrate

· need positive control: FRESH sample with and without gold coating, before and after reduction to be conclusive
· SERS substrate Glycine test
· BU (Ranjith’s) substrate: Could observe narrow and focused peak at 1400 1/cm Raman shift
· My substrate: 

1. Beaker reduced: wide peak at 1400 1/cm, as if direct SERS on glass slide

2. Chip reduced: unknown peaks at 1500 1/cm, which Ranjith had not seen and could not identify

· SEM on glycine tested substrate

· Attempted to look at chip reduced glycine tested substrate: surface appeared to be very crowded with Au particles – too much reduction and overly grown?

· 2nd attempt to look at beaker reduced and Ranjith’s BU sample: SEM showed grey screen and wouldn’t image at all (notified Anlee about it) =(
· MSSA SERS signal detection (first time on this strain)
· ATCC #25904 was purchased and hydrated for 24hr in BHI media, followed by an 6 hr inoculation in fresh BHI media

· The DI water suspension had a milky appearance

· Image with phase contrast showed very tiny cells with lots of aggregates

· Less mobile in high concentration in BHI media than diluted in DI water

· Looked for a peak at 730 1/cm Raman shift

· Unstable signal from dilution 0

· Stable signal was obtained from diluted sample (from 300ul of dilution 0 to 1.5ml of dilution 1 with DI water)
· Static: 1% laser power (2.5mW at 10%), 1s exposure time, centered at 730 1/cm; Extended: 1%, 20s, 200-1800 1/cm

· According to Ranjith, we saw unusually sharp peaks at 730, which was distinct from old strain ordered in Feb


	· MSSA dilution test (Monday-Tuesday)
· prepare BHI gel plates for CFU count
· dilute 10x each until cannot see SERS signal
· Make new batch of SERS substrate 
· with open well
· with shorter reduction time, 
· run glycine test, and
· SEM/AFM
· Hot emboss new in-situ chips 
· with thin cover slip, 
· aligned inlet/outlet holes
· Prepare abstract and drawings for CIMIT conference poster 
· Might not have time for: SERS test on BASterne spiked blood sample (with Ranjith, if both of us are available, otherwise, wait for Alexis)


\\eng-research.bu.edu\research\eng_research_klapperich\Jane\plansNaction\7July28 
All files and images are stored in these folders
[image: image1.jpg]



Image from AFM

[image: image8.jpg]


[image: image2.png]Photon count

25000

20000

15000

10000

5000

200

400

600

800 1000 1200
Raman Shift (1/cm)

1400

1600

1800

2000





SERS on Glycine on BU substrate

[image: image3.jpg]can measurement

Fle Edt View Measwement Lvevideo Anslysis Processng Procedues Toos Window Help

DERBZEY E S | €0 & % %o

[ HHEERO

A= ol kterl BREERE - EE
=

1200

B0 0 10 1600

Reman shift / o1

Completed
start

(] ) %0, 700,20 x 56285, y 98164 hidioe

&)L





SERS on Glycine on my chip-reduced substrate

[image: image4.jpg]le scan measurement.

Fle Edt View Measwement Lvevideo Anslysis Processng Procedues Toos Window Help

(EHEERED

|
JWD&BE!BEG | €0 & % %o

PE=% A= Soldter BEREE-EE
Py -

oo 30 0 10

Reman shift / o1

Completed
start

%0.,10., 20 x32.56,y 53.21 hi310s





SERS on Glycine on my beaker-reduced substrate

[image: image5.png]



[image: image6.png]> 5™, N 3
-
\ . &
L "“ Y
i ¥ . ®,
4 " & %
™ %
o - -
. - K5 N
3 6 P L
B ¥ 4
i . 5 ‘h\ 1
. - §
% N ~
. -
~ % -
. . «
4 1 a 4
™ 5
" » - . .
“ 4 %
il ’ 1
- " - -
y 5 » 3
< N o e A
- - e
% ) %
N . “ o
5 L)

200 nm Mag= 2000 KX EHT = 1.00 kv Signal A = SE2 Signal B = InLens
WD = 3.7 mm Aperture Size = 30.00 ym StageatT= 0.0° Date :24 Jul 2008





SEM on my chip-reduced substrate after Glycine test
[image: image7.jpg]can measurement

Fle Edt View Measwement Lvevideo Anslysis Processng Procedues Toos Window Help

DERBZEY E S | €0 & % %o

[ HHEERO

A= ol kterl BREERE - EE
=

00

6

70 om0 om 1000

Reman shift / o1

Completed
start

L) 0.0, 0.0, 20,0 x204.95, y 3461 41 hi3iod

o





SERS on MSSA on BU substrate

